Bonding Agent Governs Plain-Bar Pull-Out in Weak Concrete; Cast-In GFRP Bars Reach a Diameter-Independent Load Plateau

Piyarat Paoleng1, Siriphat Maneekeaw1, Sirisak Kongsomsaksakul1, Krairoj Mahannopkul1, Ittipon Meepon1,*

1 Department of Teacher Training in Civil Engineering, Faculty of Technical Education, King Mongkut’s University of Technology North Bangkok, Bangkok 10800, Thailand [TO CONFIRM: affiliation and department name for each author]

* Corresponding author: Ittipon Meepon, ittipon.m@fte.kmutnb.ac.th

ORCID: P. Paoleng 0009-0008-5332-1007; S. Maneekeaw 0009-0002-0435-2866; S. Kongsomsaksakul 0009-0001-2352-5550; K. Mahannopkul 0000-0002-6207-0958; I. Meepon 0000-0001-5353-3511

# Abstract

Load passes between a reinforcing bar and concrete through the bar surface, so interface strength decides how repaired and new members perform. Much existing building stock in developing regions uses concrete weaker than codes assume, and retrofit crews anchor bars in drilled holes with whichever epoxy, grout or mortar is at hand. Pull-out data for such concrete are scarce, most of all for glass fibre-reinforced polymer (GFRP) bars, and it is unclear which bonding agent works and how bond scales with bar size. Here we show, from 180 pull-out tests on 150 mm cubes (nominal strength 4.9–23.5 MPa), that the bonding agent explains most of the variation in bond stress of post-installed plain steel bars (partial η² = 0.73): epoxy averaged 1.88 MPa, non-shrink grout 0.43 MPa and cement mortar 0.02 MPa, and epoxy outperformed grout only from 14.7 MPa upward (agent × strength F(4, 108) = 23.2, p < 0.001). Cast-in GFRP bars of 6, 9 and 12 mm scaled weakly with diameter (power-law exponent 0.01–0.47, against 1 for uniform interface stress) and gained no load between 14.7 and 23.5 MPa (pooled mean 20.8 kN), so apparent bond stress fell with diameter, a pattern the ACI 440.1R-06 expression does not reproduce. Cement mortar was ineffective on plain bars. Concrete strengths were nominal grades (companion cubes were not crushed in the original tests) and each group had only five specimens, so the values are indicative only; design use requires tests on the actual bar–agent–concrete combination.

Keywords: bond strength; pull-out test; post-installed plain bars; bonding agent; GFRP bar; low-strength concrete

# 1. Introduction

A reinforcing bar carries load only as far as its surface can pass force to the surrounding concrete. That transfer combines chemical adhesion, friction, and the bearing of concrete against ribs or other surface features [1, 2], and the balance among the three depends on the bar. A plain round bar has no ribs, so its pull-out resistance rests on adhesion and friction alone [3], and the material at the interface matters more than it does for a ribbed bar. Design rules reflect the split: the development-length provisions of ACI 318 were built on test databases of ribbed bars [4, 5], and a separate model for straight plain bars has appeared only recently [6].

Bond matters most where concrete is weak. Reconnaissance after the 2010 Haiti earthquake tied much of the building damage to low-strength concrete and poor construction practice [7]; the role of construction materials in building collapses has been examined for the 2016 Ecuador earthquake [8]; and concrete-quality problems in multistorey construction have been documented in Ghana [9]. Core and non-destructive testing has been used to characterise low-strength concrete in existing structures [10], and bond of steel bars in concrete of 5–30 MPa has recently been studied in the context of CFRP confinement [11]. Repair and strengthening of such buildings often depend on bars installed in drilled holes, and the material that fills the annulus is frequently chosen for cost and availability rather than for measured bond capacity.

Comparisons of bonding agents for post-installed bars come mostly from ribbed bars, and they favour epoxy. Tayeh et al. reported higher bond for chemical adhesives than for cement-based binders in their test series [12]. Ahmed et al. tested 108 high-strength bars set in epoxy and described their bond strength with a square-root function of concrete strength [13], and Fayed et al. attributed the higher capacity of ribbed bars over threaded bars to better interlock [14]. Other studies varied the host concrete or the anchor itself, examining concrete containing marble powder and glass fibre [15], post-installed anchors under axial tension [16], and cement mortars with supplementary cementitious materials designed for anchoring post-installed bars [17].

Cementitious grout has mostly been studied as a filler around bars in ducts and splice sleeves, or as a high-strength anchoring medium. Examples include the bond strength of grouted bars [18], bars grouted in ducts [19], the confining effect of grouted splice sleeves [20], bond–slip models of high-strength grout and of the steel–grout interface in sleeve couplers [21, 22], machine-learning prediction of anchor-bolt–grout bond [23], anchorage of SBPDN bars in high-strength grout mortar [24], and microbial cement grout [25]. In the literature we located, no study put plain round bars, epoxy, non-shrink grout, and ordinary cement mortar through one protocol in concrete weaker than 25 MPa. That search was targeted rather than systematic, so the statement records our best knowledge and not an exhaustive claim.

GFRP bars pose a separate question. Pull-out and development-length studies of these bars are numerous [26–29] and have been summarised in reviews [30, 31], but the studies we located used concrete of normal or high strength [32, 33]; the lowest strength we found in a GFRP pull-out study was 20.4 MPa [34]. Design guidance for FRP bars expresses bond strength through cover-to-diameter and diameter-to-embedment terms [35, 36], and we found no pull-out data that would test that expression in concrete below 15 MPa.

We therefore tested 180 specimens under a single pull-out protocol and asked three questions. First, how do epoxy, non-shrink grout, and cement mortar rank as anchoring agents for post-installed plain round bars in concrete of 4.9–23.5 MPa, and does the ranking depend on concrete strength? Second, how does bond stress in these bars scale with concrete strength and bar diameter, and where does the capacity of the bar itself begin to limit the result? Third, how do cast-in GFRP bars behave over the same strength range, and how does their apparent bond stress compare with the ACI 440.1R-06 expression and with the plain bars? The specimens come from two student research projects supervised by the authors, which share a protocol but were not designed as one factorial experiment; Section 2.1 states what that means for inference.

# 2. Experimental programme

## 2.1 Test matrix and provenance of the data

Two bar systems were tested under one protocol (Table 1, Fig. 1). Plain round steel bars of 6, 9, and 12 mm (RB6, RB9, RB12) were post-installed in drilled holes with epoxy, non-shrink grout, or cement mortar, and GFRP bars of 6, 9, and 12 mm were cast into the concrete. Each bar was pulled from a 150 mm concrete cube with a bonded length le = 140 mm. Nominal concrete strengths were 4.9, 14.7, and 23.5 MPa (50, 150, and 240 ksc). Five specimens per group gave 135 plain-bar specimens (3 diameters × 3 agents × 3 strengths × 5) and 45 GFRP specimens (3 diameters × 3 strengths × 5), 180 in all.

The specimens were prepared and tested in the civil engineering laboratories of King Mongkut’s University of Technology North Bangkok as two undergraduate special projects supervised by the authors, one on plain steel bars and one on GFRP bars. The analysis reported here was redone from specimen-level records and not taken from the summary tables of the project reports. [TO CONFIRM: origin and test date of the fifth specimen in every plain-bar group, and of the repeated GFRP tests, which replace or extend the values in the original GFRP project report; confirm that the procedure was unchanged.]

Three features of this origin limit inference and are carried through the paper. First, the GFRP series differs from the plain-bar series in installation (cast-in rather than post-installed) and has no bonding agent, so comparisons between the two series are descriptive and the inferential analysis is confined to the plain-bar series, where agent, diameter, and strength are fully crossed. Second, no analysis was specified before the data were examined, so the p values are descriptive measures of how unusual a difference is and not error-controlled tests. Third, concrete strengths are nominal grades and were not checked on companion cubes (Section 2.2).

[REVISION – reviewer comment 2] The origin of every specimen is to be documented in a traceability log (Table S5); groups without supporting records are to be removed from the analysis.

Table 1. Test matrix.

| Series | Bar | Diameters (mm) | Installation | Bonding agent | Nominal f′c (MPa) | Groups × n | Specimens |
| --- | --- | --- | --- | --- | --- | --- | --- |
| RB | Plain round steel | 6, 9, 12 | Post-installed | Epoxy, non-shrink grout, cement mortar | 4.9, 14.7, 23.5 | 27 × 5 | 135 |
| GFRP | GFRP bar | 6, 9, 12 | Cast-in | None | 4.9, 14.7, 23.5 | 9 × 5 | 45 |
| Total |  |  |  |  |  | 36 groups | 180 |

Fig. 1. Experimental programme and analysis workflow. Plain steel bars were post-installed in drilled holes and GFRP bars were cast in; all 180 specimens were pulled out in the same test arrangement and analysed with the same data-reduction rules. [REVISION – dashed boxes mark the verification steps requested in review (Appendix S). Keep only the steps actually completed; TO CONFIRM.]

## 2.2 Materials

Steel bars. Plain round bars were of the grade designated SR24 in the project report; nominal diameters were used throughout. For this designation, a supplier’s product-standard sheet lists a minimum yield strength of 235 MPa and a minimum tensile strength of 385 MPa under TIS 20-2559, whereas the project report cites TIS 20-2527. We use 235 MPa only as a reference level for the bar stress in Section 2.5; yield strength was not measured. [TO CONFIRM: measured yield and tensile strength, supplier, and the edition of TIS 20 that applies; check the quoted values against the standard itself.]

[REVISION – reviewer comment 7] Tensile coupons of each bar size are to be tested; Table S2 shows the layout with PLACEHOLDER values. Sections 3.4 and 4.3 must be rewritten once measured yield strengths replace the catalogue value.

GFRP bars. Bars of 6, 9, and 12 mm were tested. One end of each bar was grouted with non-shrink grout inside a steel tube to give a grip for the testing machine. The surface treatment, fibre content, and tensile properties of the bars are not documented in the source. [TO CONFIRM: manufacturer, surface type, tensile strength and modulus of the three sizes.]

[REVISION – reviewer comment 7] Manufacturer data and tensile properties of the GFRP bars are to be reported (Table S3, PLACEHOLDER values).

Concrete. All mixtures were made from one commercial pre-blended dry-mix concrete supplied in bags (nominal grades 50, 150, and 240 ksc). The 4.9 MPa mixture diluted the dry mix with an equal mass of coarse sand (2.00–4.75 mm), the 14.7 and 23.5 MPa mixtures used the undiluted dry mix, and the last two differ only in the recorded curing period, 7 d and 14 d (Table 2). Cubes for the GFRP series used 5–6 L of water per bag of dry mix. Compressive strength was not measured on companion cubes in either project, so the strengths quoted in this paper are nominal grade labels and not measured values; the possible consequences are discussed in Section 4.2.

[REVISION – reviewer comment 1] Companion 150 mm cubes from each mixture are to be crushed at the age of the pull-out test. Table S1 shows the layout with PLACEHOLDER values only. Nominal grades are retained throughout the paper until measured values exist.

Table 2. Concrete mixtures used for the plain-bar series, as recorded in the source project (batch masses).

| Nominal strength | Dry-mix concrete (kg) | Water (kg) | Coarse sand (kg) | Curing period (d) |
| --- | --- | --- | --- | --- |
| 4.9 MPa (50 ksc) | 150 | 50 | 150 | 5 |
| 14.7 MPa (150 ksc) | 300 | 48 | – | 7 |
| 23.5 MPa (240 ksc) | 300 | 48 | – | 14 |

For the GFRP series the source records 5–6 L of water per bag of dry mix and immersion curing; the bag mass and the curing period are not documented. [TO CONFIRM]

Bonding agents. The epoxy was a two-component, solvent-free adhesive (resin and hardener) that gives a grey paste. The non-shrink grout was a ready-mixed cementitious product containing cement, graded sand, and admixtures, for which the project report quotes manufacturer-declared compressive strengths above 300 ksc at one day and above 850 ksc (about 29 and 83 MPa). The cement mortar was a bagged, ready-mixed product of cement, sand, and admixture. [TO CONFIRM: product names, water–powder ratios, and flow or consistency of the grout and mortar, none of which is recorded.]

## 2.3 Specimen preparation

Cubes of 150 mm were cast in oiled moulds in three layers, each rodded 25 times. For the plain-bar series, a wooden dowel was pressed into the centre of the fresh concrete to mark the hole and withdrawn after about one hour. The cubes were demoulded after 24 h. A hole was then drilled along the dowel line, the bar was coated by dipping it in the freshly mixed agent and was then pushed into the hole, and the specimen was left for two to three days before testing (Fig. 2). [TO CONFIRM: drill-bit diameter, hole depth relative to the 150 mm cube, hole cleaning, and how the annulus was filled; the report describes dipping the bar in the agent, not injecting the agent into the hole.]

For the GFRP series, each bar was held vertically at the centre of the mould by a perforated timber plate (150 × 150 × 10 mm) that also let the free end project for the displacement transducer. Concrete was placed and rodded as above, a second plate locked the bar position at the top, the cubes were demoulded after 24 h and immersed in water. [TO CONFIRM: immersion period and test age.]

Fig. 2. Specimen and test arrangement. (a) Schematic of the pull-out specimen (bonded length 140 mm in a 150 mm cube; the loaded end is at the bottom and slip is read at the free end). Hatching: dots, concrete; diagonal lines, steel bar; cross-hatching, bonding agent. GFRP bars were cast in place, without a bonding-agent annulus. (b) Forming the hole position with a wooden dowel in fresh concrete. (c) Drilling the hole. (d) Bar bonded in place with the free end projecting. (e) Displacement transducer (LVDT) at the free end. Panels (b)–(e) are photographs from the source project. [TO CONFIRM: block height and hole depth in (a); written permission of the students for the photographs.]

## 2.4 Pull-out test

Each cube was tested in direct pull-out in a universal testing machine following the ASTM C234 procedure adopted in the source projects [37]. The bar was gripped at its loaded end while the cube bore against a reaction plate, and a linear variable differential transformer (LVDT) at the unloaded end recorded slip. The peak load P was taken as the pull-out capacity of the specimen. [TO CONFIRM: machine capacity, loading rate or displacement rate, reaction arrangement, and age at testing.] Load–slip records are not analysed in this paper. Failure mode was recorded after testing, for one representative specimen per group in the plain-bar series (27 groups) and for every specimen in the GFRP series.

[REVISION – reviewer comment 4] A supplementary series with le = 5 db (geometry of ACI 440.3R, Annex B.3) is laid out in Table S4 with PLACEHOLDER values, and load–slip curves from the LVDT records are to be added [TO CONFIRM that the records exist].

The arrangement departs from the pull-out specimen of ACI 440.3R-04, Annex B.3 (a 200 mm cube with a bonded length of five bar diameters) [38], and ASTM withdrew C234 in 2000 and issued no direct successor. The ratio le/db ranged from 11.7 (12 mm bars) to 23.3 (6 mm bars), so the bond stress reported below is a stress averaged over a long bonded length. Section 4.6 returns to this.

## 2.5 Data reduction

Average bond stress was computed from the peak load and the nominal bar diameter db,

τ=Pπdble	(1)

and a strength-normalised value N was obtained by dividing by the square root of the nominal concrete strength (MPa units),

N=τf'c	(2)

The nominal stress in the bar at peak load was also computed,

σb=4Pπdb2	(3)

and compared with the catalogue minimum yield strength of SR24 (235 MPa, Section 2.2). The comparison is a screening device and not a measurement. A value above 235 MPa does not prove that the bar yielded, because the real yield strength is unknown and usually exceeds the specified minimum; it does show that the bar, and not the interface, could have set the limit, in which case τ is a lower bound on the interface strength.

For the GFRP series, measured N was compared with the bond-strength expression of ACI 440.1R-06 [35] in the form quoted by Shbeeb et al. [36],

τf'c=0.33 + 0.025cdb+ 8.3dble	(4)

where c is the concrete cover (mm) and le replaces the embedment length. We assumed c = (150 − db)/2, the distance from the bar surface to the nearest cube face. The source we used states no upper limit on c/db, so predictions are reported without a cap, and a cap of 3.5 is shown as a sensitivity check in Section 3.7.

Specimens in which the bar slid out with no recorded resistance (P = 0) were kept in every analysis as zeros, because they are the outcome of interest. Their effect on the main results was checked separately (Section 3.2).

## 2.6 Statistical analysis

Bond stress in the plain-bar series was analysed with a three-factor ANOVA (agent, diameter, and nominal strength) fitted to all 135 specimens. Type III tests used effects (sum-to-zero) coding, and partial eta squared (ηp2) is reported as the effect size. Because many groups contained zeros and the variances were unequal, the agent × strength and agent × diameter interactions were re-tested with a Freedman–Lane permutation test (4,000 permutations), heteroscedasticity-consistent (HC3) Wald tests, square-root, log(τ + 0.1), and rank transformations, the first four specimens of each group, and the exclusion of the one group whose representative specimen split. Pairwise contrasts between agents used Welch t-tests with Hedges’ g, and a Mann–Whitney test where the outcome was borderline. Trends with strength and diameter were summarised by Spearman correlation and Kruskal–Wallis tests within each agent, and the proportions of zero-load specimens were compared with Fisher’s exact test.

For the GFRP series, two-way ANOVA (diameter × strength; 36 error degrees of freedom) was applied to P, τ, and N. The scaling of capacity with diameter, in both series, was described by a log–log fit of the form

P=kdbb	(5)

within each strength for GFRP bars, and with strength as a fixed effect for plain bars with positive load. An exponent b = 1 corresponds to a uniform stress over the bar perimeter, b = 2 to a capacity proportional to bar area, and b = 0 to a capacity that does not depend on diameter. No multiplicity correction was applied. Computations were done in Python (NumPy, SciPy) on the specimen-level data.

# 3. Results

## 3.1 Effect of the bonding agent

Table 3 gives the bond stress of the plain-bar series by agent and strength, and Fig. 3 shows every group. Pooled over diameters and strengths (n = 45 per agent), epoxy averaged 1.88 ± 1.64 MPa (mean ± SD), non-shrink grout 0.43 ± 0.44 MPa, and cement mortar 0.021 ± 0.055 MPa. Epoxy exceeded grout by 1.45 MPa (Welch p < 0.001, Hedges’ g = 1.19; Mann–Whitney p < 0.001), and grout exceeded mortar by 0.41 MPa (p < 0.001, g = 1.28; Table 4). The highest bond stress of any mortar specimen was 0.27 MPa, against 1.58 MPa for grout and 5.75 MPa for epoxy; the corresponding peak loads were 1.05, 6.3, and 30.3 kN.

Specimens that recorded no load were frequent with the weaker agents: 36 of 45 with mortar, 16 of 45 with grout, and 6 of 45 with epoxy (Fig. 4c). The proportion of zero-load specimens differed between epoxy and grout (Fisher exact p = 0.03) and between grout and mortar (p < 0.001).

Table 3. Bond stress τ (MPa) of the plain-bar series by bonding agent and nominal concrete strength, mean (SD).

| Agent | 4.9 MPa | 14.7 MPa | 23.5 MPa | All strengths | Zero load, of 45 | Highest τ |
| --- | --- | --- | --- | --- | --- | --- |
| Epoxy | 1.00 (1.37) | 1.50 (0.86) | 3.13 (1.78) | 1.88 (1.64) | 6 | 5.75 |
| Non-shrink grout | 0.55 (0.54) | 0.37 (0.50) | 0.37 (0.23) | 0.43 (0.44) | 16 | 1.58 |
| Cement mortar | 0.00 (0.00) | 0.04 (0.08) | 0.03 (0.04) | 0.02 (0.05) | 36 | 0.27 |

Each strength cell pools the three diameters (n = 15); the last columns pool all 45 specimens per agent. Zero-load specimens are included as zeros.

Fig. 3. Bond stress τ of the plain-bar series against nominal concrete strength for (a) RB6, (b) RB9, and (c) RB12. Symbols are group means ± 1 SD (n = 5); error bars are omitted for cement mortar, whose SD is below 0.1 MPa and smaller than the symbol. [AUTHORS: re-plot Figs 3–5 and 9 from the raw specimen file before submission; the group SDs in v3 were transcribed from the v2 figure and checked against Table 3.]

Table 4. Pairwise contrasts between bonding agents in the plain-bar series.

| Contrast (first minus second) | n per group | Mean difference (MPa) | Welch t | p | Hedges’ g | Mann–Whitney p |
| --- | --- | --- | --- | --- | --- | --- |
| Epoxy − grout, all strengths | 45 | 1.45 | 5.71 | < 0.001 | 1.19 | < 0.001 |
| Epoxy − mortar, all strengths | 45 | 1.86 | 7.58 | < 0.001 | 1.58 | < 0.001 |
| Grout − mortar, all strengths | 45 | 0.41 | 6.14 | < 0.001 | 1.28 | < 0.001 |
| Epoxy − grout at 4.9 MPa | 15 | 0.45 | 1.18 | 0.25 | 0.42 | 0.97 |
| Epoxy − grout at 14.7 MPa | 15 | 1.13 | 4.41 | < 0.001 | 1.57 | < 0.001 |
| Epoxy − grout at 23.5 MPa | 15 | 2.76 | 5.95 | < 0.001 | 2.11 | < 0.001 |
| Grout − mortar at 4.9 MPa | 15 | 0.55 | 3.94 | 0.001 | 1.40 | < 0.001 |
| Grout − mortar at 14.7 MPa | 15 | 0.33 | 2.54 | 0.02 | 0.90 | 0.08 |
| Grout − mortar at 23.5 MPa | 15 | 0.34 | 5.71 | < 0.001 | 2.03 | < 0.001 |

No multiplicity correction was applied. The epoxy–grout contrast at 4.9 MPa is the only one in the table whose Welch and Mann–Whitney tests both fail to separate the groups.

## 3.2 Dependence on concrete strength and stability of the result

The ranking of the agents depended on the concrete strength (agent × strength F(4, 108) = 23.2, p < 0.001, ηp2 = 0.46; Table 5 and Fig. 4a). Epoxy gave 1.00, 1.50, and 3.13 MPa at 4.9, 14.7, and 23.5 MPa, whereas grout gave 0.55, 0.37, and 0.37 MPa. At 4.9 MPa the two agents could not be separated (difference 0.45 MPa, p = 0.25, g = 0.42; Mann–Whitney p = 0.97). At 14.7 and 23.5 MPa epoxy exceeded grout by 1.13 MPa (p < 0.001, g = 1.57) and 2.76 MPa (p < 0.001, g = 2.11), which is 4.1 and 8.5 times the grout mean (1.8 times at 4.9 MPa). Grout exceeded mortar at every strength, but by only 0.33–0.55 MPa (Table 4).

Table 5. Three-factor ANOVA of bond stress τ for the plain-bar series (n = 135 specimens; Type III, effects coding).

| Effect | df | F | p | ηp2 |
| --- | --- | --- | --- | --- |
| Agent | 2, 108 | 149.3 | < 0.001 | 0.734 |
| Diameter | 2, 108 | 20.1 | < 0.001 | 0.271 |
| Nominal f′c | 2, 108 | 19.5 | < 0.001 | 0.265 |
| Agent × diameter | 4, 108 | 18.0 | < 0.001 | 0.400 |
| Agent × f′c | 4, 108 | 23.2 | < 0.001 | 0.462 |
| Diameter × f′c | 4, 108 | 5.9 | < 0.001 | 0.179 |
| Agent × diameter × f′c | 8, 108 | 8.7 | < 0.001 | 0.391 |

The agent effect was the largest (ηp2 = 0.73), and diameter and strength each had a moderate effect (ηp2 = 0.27 and 0.26). All interactions were significant, including the three-way term (F(8, 108) = 8.7, ηp2 = 0.39), so the effects of strength and diameter were not the same for the three agents.

Table 6 lists the checks applied to the two interaction terms. The agent × strength interaction remained significant under every analysis, including the rank transformation, and it survived when the comparison was reduced to epoxy and grout with or without the zero-load specimens. It is therefore not a product of zero inflation, unequal variance, or the one group with a splitting failure. The agent × diameter interaction held in all but one analysis; under the rank transformation it was not significant (p = 0.14), so it is the less secure of the two.

Table 6. Stability of the two agent interactions.

| Analysis | n | Agent × strength | p | Agent × diameter | p |
| --- | --- | --- | --- | --- | --- |
| Primary model (all specimens) | 135 | F(4, 108) = 23.2 | < 0.001 | F(4, 108) = 18.0 | < 0.001 |
| Freedman–Lane permutation (4,000 permutations) | 135 | F = 23.2 | 0.00025 | F = 18.0 | 0.00025 |
| HC3 Wald test | 135 | χ²(4) = 39.5 | < 0.001 | χ²(4) = 33.4 | < 0.001 |
| Square-root transform of τ | 135 | F(4, 108) = 11.3 | < 0.001 | F(4, 108) = 6.9 | < 0.001 |
| log(τ + 0.1) transform | 135 | F(4, 108) = 8.3 | < 0.001 | F(4, 108) = 3.8 | 0.007 |
| Rank transform of τ | 135 | F(4, 108) = 5.5 | < 0.001 | F(4, 108) = 1.8 | 0.14 |
| First four specimens of each group | 108 | F(4, 81) = 14.3 | < 0.001 | F(4, 81) = 11.5 | < 0.001 |
| Split-group representative specimen excluded | 134 | F(4, 107) = 22.8 | < 0.001 | F(4, 107) = 17.7 | < 0.001 |
| Epoxy and grout only | 90 | F(2, 84) = 9.9 | < 0.001 | – | – |
| Epoxy and grout only, zero-load specimens excluded | 68 | F(2, 62) = 9.7 | < 0.001 | – | – |

The smallest attainable permutation p value with 4,000 permutations is 0.00025.

Fig. 4. Dependence of bond stress on agent, strength, and diameter in the plain-bar series. (a) Mean τ with 95% confidence intervals by agent and nominal strength (n = 15 per point). (b) Mean τ with 95% confidence intervals by agent and bar diameter (n = 15 per point). (c) Share of specimens that recorded zero load, by agent and strength (n = 15 per bar). Bar colour and hatching in (c) follow the agent legend in (a): epoxy, oblique lines; grout, dots; mortar, cross-hatching.

## 3.3 Effect of strength and diameter within each agent

Strength mattered for epoxy and not for grout. Epoxy bond stress rose with nominal strength from 1.00 to 3.13 MPa (Spearman ρ = 0.51, p < 0.001; Kruskal–Wallis p = 0.003), and grout showed no trend (0.55, 0.37, and 0.37 MPa; ρ = −0.07, p = 0.64). Mortar showed a weak rank correlation (ρ = 0.34, p = 0.02), but its means stayed at 0.00, 0.04, and 0.03 MPa.

Diameter followed the same pattern for epoxy, whose bond stress was 1.17, 1.40, and 3.06 MPa for RB6, RB9, and RB12 (Spearman ρ = 0.46, p = 0.002; Kruskal–Wallis p = 0.006; Fig. 5a). Grout (0.31, 0.52, and 0.45 MPa; p = 0.28) and mortar (0.00, 0.04, and 0.02 MPa; p = 0.06) showed no clear diameter effect. The epoxy effect was not uniform across strengths. RB12 gave 2.61, 1.33, and 5.23 MPa at 4.9, 14.7, and 23.5 MPa, against 0.17, 1.15, and 2.19 MPa for RB6 and 0.20, 2.02, and 1.98 MPa for RB9, so the gain came from RB12 at the lowest and highest strengths, and RB9 showed no change between 14.7 and 23.5 MPa.

Fig. 5. Epoxy-anchored plain bars. (a) Bond stress τ and (b) nominal bar stress at peak load σb against bar diameter for each nominal strength (mean ± 1 SD, n = 5). The dashed line in (b) is the catalogue minimum yield strength of SR24 bar (235 MPa), which was not measured.

## 3.4 Bar stress at peak load and scaling of capacity with diameter

For epoxy, the nominal bar stress at peak load reached or exceeded the catalogue yield level in part of the series (Fig. 5b). Group means of σb were 16, 107, and 204 MPa for RB6, 13, 126, and 123 MPa for RB9, and 122, 62, and 244 MPa for RB12 at 4.9, 14.7, and 23.5 MPa. Eight of 45 epoxy specimens exceeded 235 MPa (1 at 14.7 MPa and 7 at 23.5 MPa; 4 of the RB6 and 4 of the RB12 bars), with a maximum of 350 MPa (RB6, 23.5 MPa). The mean peak load of RB12 at 23.5 MPa (27.6 kN) was 104% of the load that 235 MPa would give (26.6 kN). Grout and mortar never came close to this level: the highest bar stress was 138 MPa with grout and 17 MPa with mortar.

A log–log fit of peak load against diameter, using the specimens with positive load and strength as a fixed effect, gave an exponent b = 2.12 (95% half-width 0.90, n = 39) for epoxy. That value is larger than the b = 1 of a uniform interface stress and is compatible with b = 2, a capacity proportional to bar area. For grout the exponent was 0.38 (half-width 0.84, n = 29), which the data cannot distinguish from 0 or from 1.

## 3.5 Failure modes

One failure mode was recorded per plain-bar group (Fig. 6a). Epoxy groups failed by pull-out (7 groups) or by pull-out with bar yielding (2; RB12 at 4.9 and at 23.5 MPa). Grout groups failed by interface slip (6), by interface slip with splitting (1; RB12 at 23.5 MPa), or by zero-bond slip-out, in which the bar was withdrawn without recorded resistance (2). Mortar groups failed by zero-bond slip-out (5) or by slip inside the mortar layer, recorded as mortar shear slippage (4). These counts refer to groups, each represented by a single specimen, so they indicate the dominant behaviour and not the frequency among specimens.

Fig. 6. Failure modes. (a) Mode recorded for each of the nine groups per agent in the plain-bar series (one representative specimen per group). (b) GFRP specimens (n = 15 per strength) that failed by splitting of the cube or by pull-out and slip.

## 3.6 GFRP bars

Table 7 lists the nine GFRP groups. Within-group coefficients of variation of peak load were 2.0–7.2% at 4.9 and 14.7 MPa and 5.3–18.9% at 23.5 MPa. Peak load rose with diameter at 4.9 MPa (11.1, 14.5, and 15.3 kN for 6, 9, and 12 mm; power-law exponent b = 0.47 with a 95% half-width of 0.10, R² = 0.90), was independent of diameter at 14.7 MPa (21.4, 20.8, and 21.7 kN; b = 0.01 ± 0.10; one-way F = 0.85, p = 0.45), and increased with diameter again at 23.5 MPa, although not uniformly across diameters (17.9, 19.1, and 23.8 kN; b = 0.41 ± 0.29; p = 0.010 for the diameter effect) (Fig. 7a). With a uniform interface stress b would equal 1, so no strength level behaved that way.

Table 7. Cast-in GFRP bars: peak load and derived bond measures (n = 5 per group).

| db (mm) | Nominal f′c (MPa) | P mean (SD), kN | CV of P (%) | P range (kN) | τ mean (MPa) | N mean | Splitting, of 5 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 6 | 4.9 | 11.1 (0.2) | 2.0 | 10.9–11.3 | 4.21 | 1.90 | 0 |
| 6 | 14.7 | 21.4 (0.7) | 3.2 | 20.4–22.2 | 8.11 | 2.11 | 3 |
| 6 | 23.5 | 17.9 (2.6) | 14.3 | 14.3–20.4 | 6.77 | 1.40 | 3 |
| 9 | 4.9 | 14.5 (0.4) | 2.9 | 14.1–15.0 | 3.66 | 1.65 | 2 |
| 9 | 14.7 | 20.8 (0.7) | 3.4 | 19.9–21.7 | 5.26 | 1.37 | 3 |
| 9 | 23.5 | 19.1 (3.6) | 18.9 | 14.9–24.2 | 4.82 | 0.99 | 3 |
| 12 | 4.9 | 15.3 (0.6) | 4.1 | 14.4–16.1 | 2.90 | 1.31 | 3 |
| 12 | 14.7 | 21.7 (1.6) | 7.2 | 19.9–23.4 | 4.11 | 1.07 | 3 |
| 12 | 23.5 | 23.8 (1.3) | 5.3 | 22.6–25.8 | 4.51 | 0.93 | 3 |

τ = P/(πdble) with nominal diameters; N = τ/√f′c.

Fig. 7. Effect of diameter on GFRP pull-out capacity. (a) Peak load against bar diameter on logarithmic axes; symbols are group means ± 1 SD, translucent vertical bars are the minimum–maximum range of the five specimens, and dashed lines are the fitted power laws with exponent b in the legend (b = 1 for uniform interface stress, b = 0 for a diameter-independent capacity). (b) Apparent bond stress; the dotted curve is the stress that a constant load equal to the pooled mean peak load at 14.7 and 23.5 MPa would give.

At the upper end of the range, strength stopped affecting the GFRP bars. Between 4.9 and 14.7 MPa, mean peak load rose by factors of 1.93, 1.44, and 1.42 for the 6, 9, and 12 mm bars (all p < 0.001), against 1.73 expected if capacity followed the square root of strength. Between 14.7 and 23.5 MPa it changed by factors of 0.84 (p = 0.035), 0.92 (p = 0.34), and 1.10 (p = 0.045), a change whose sign differs among the three diameters. Pooled over the two higher strengths and all diameters, peak load was 20.8 ± 2.7 kN (CV 12.9%, range 14.3–25.8 kN, n = 30), and the means at 14.7 and 23.5 MPa did not differ (21.3 versus 20.3 kN, Welch p = 0.30, g = −0.38) (Fig. 8a).

Two-way ANOVA (Table 8) found significant effects of diameter, strength, and their interaction on peak load, apparent bond stress, and normalised bond. Because the load plateau spans a fourfold range of bar area, τ and N fall with diameter: at 14.7 MPa, τ was 8.11, 5.26, and 4.11 MPa and N was 2.11, 1.37, and 1.07 for the 6, 9, and 12 mm bars. Splitting of the cube was recorded in 23 of 45 specimens (5 of 15 at 4.9 MPa and 9 of 15 at both 14.7 and 23.5 MPa; Fig. 6b), and peak load at 14.7 and 23.5 MPa did not depend on failure mode (20.6 kN with splitting, n = 18; 21.1 kN without, n = 12; p = 0.72). At the maximum load, the nominal stress in the bar was 786 MPa for the 6 mm bar (P = 22.23 kN), 380 MPa for the 9 mm bar (24.18 kN), and 228 MPa for the 12 mm bar (25.76 kN).

Table 8. Two-way ANOVA of the GFRP series (n = 45).

|  |  | Peak load P |  | Bond stress τ |  | Normalised bond N |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Effect | df | F | ηp2 | F | ηp2 | F | ηp2 |
| Diameter db | 2, 36 | 16.5 | 0.478 | 110.6 | 0.860 | 175.9 | 0.907 |
| Nominal f′c | 2, 36 | 92.7 | 0.837 | 91.9 | 0.836 | 102.6 | 0.851 |
| db × f′c | 4, 36 | 5.2 | 0.365 | 12.3 | 0.578 | 13.8 | 0.604 |

All p < 0.001 except db × f′c for P (p = 0.002).

Fig. 8. Effect of nominal concrete strength on GFRP bars. (a) Peak load against strength for each diameter; the shaded band is the pooled mean ± 1 SD at 14.7 and 23.5 MPa (20.8 ± 2.7 kN). (b) Normalised bond N against strength; dashed lines are ACI 440.1R-06 predictions without a cover limit (Section 2.5).

## 3.7 Comparison with the ACI 440.1R-06 expression

Predicted N from the ACI 440.1R-06 expression is independent of strength and was 0.99, 1.06, and 1.19 for the 6, 9, and 12 mm bars (Table 9). Measured N fell with strength (mean 1.62, 1.52, and 1.11 at 4.9, 14.7, and 23.5 MPa) and with diameter, so the measured-to-predicted ratio ranged from 0.79 to 2.15. It exceeded 1 for the 6 mm bars at every strength and for the 9 mm bars at 4.9 and 14.7 MPa, and it was below 1 for the 12 mm bars at 14.7 and 23.5 MPa and for the 9 mm bars at 23.5 MPa. As a sensitivity check, limiting c/db to 3.5 lowers the predictions to 0.77, 0.95, and 1.13 and raises the ratios by up to 27%.

Table 9. Measured normalised bond of the GFRP bars against the ACI 440.1R-06 expression (Eq. 4; no cap on c/db).

|  |  |  | Measured N |  |  | Measured / predicted |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| db (mm) | c/db | Predicted N | 4.9 MPa | 14.7 MPa | 23.5 MPa | 4.9 MPa | 14.7 MPa | 23.5 MPa |
| 6 | 12.0 | 0.99 | 1.90 | 2.11 | 1.40 | 1.93 | 2.15 | 1.42 |
| 9 | 7.8 | 1.06 | 1.65 | 1.37 | 0.99 | 1.56 | 1.30 | 0.94 |
| 12 | 5.8 | 1.19 | 1.31 | 1.07 | 0.93 | 1.10 | 0.90 | 0.79 |

c = (150 − db)/2 (assumed); le = 140 mm; measured N is the group mean (n = 5).

## 3.8 Normalised bond across systems

Fig. 9a sets the four systems side by side in terms of N. Plain bars in epoxy averaged 0.45, 0.39, and 0.65 at 4.9, 14.7, and 23.5 MPa, plain bars in grout 0.25, 0.10, and 0.08, and mortar did not exceed 0.01. GFRP bars gave 1.62, 1.52, and 1.11. At matched diameter and nominal strength, the mean peak load of the GFRP bars exceeded that of the epoxy-anchored plain bars in 8 of 9 cells, by factors of 1.1 to 24.3 (Fig. 9b). The exception was the 12 mm bar at 23.5 MPa (23.8 versus 27.6 kN), where the plain bar had reached the catalogue yield level (Section 3.4). The GFRP bars were cast in and the plain bars post-installed, and the GFRP capacity does not scale with bar area (Section 3.6), so these comparisons are descriptive and should not be read as a ranking of bar types.

Fig. 9. Comparison of the plain-bar and GFRP series. (a) Normalised bond N = τ/√f′c for each system (mean ± 1 SD, n = 15 per point). (b) Mean peak load of the GFRP bars against that of epoxy-anchored plain bars at the same diameter (point labels, mm) and nominal strength; the dashed line is 1:1. GFRP bars were cast in and plain bars post-installed, so the comparison is descriptive.

# 4. Discussion

## 4.1 The bonding agent governs plain-bar capacity

The central result is that, for plain bars in weak concrete, the choice of agent outweighs the choice of diameter or strength. The agent effect (ηp2 = 0.73) was far larger than the diameter and strength effects (0.27 and 0.26), and epoxy averaged 4.4 times the grout mean and 91 times the mortar mean (Table 3). A plain bar has no ribs, so load must pass by adhesion and friction at the interface [3]. An epoxy resin can be expected to adhere chemically to both steel and concrete, whereas a cementitious agent relies more on friction and on a physical adhesion that bleeding or shrinkage at the steel surface may weaken; we did not measure either effect. This reading agrees with reports that chemical adhesives bond better than cement-based binders [12], and the failure modes point the same way: epoxy groups failed by pull-out, grout groups mostly by interface slip (6 of 9), and mortar groups by zero-bond slip-out or slip inside the mortar layer (Fig. 6a). It remains an interpretation, because no fracture surface was examined and the design does not isolate the mechanism.

The advantage of epoxy also depended on the host concrete. At 4.9 MPa epoxy and grout could not be separated, and 5 of 15 epoxy specimens recorded zero load. One possible reason is that the sand-diluted, weakest mixture gave the epoxy too friable a hole wall to bond to, but this is a hypothesis: hole condition and dust removal were not recorded. The installation method may also have influenced the ranking. Bars were dipped in the agent and pushed into the hole, which suits a fluid resin better than a stiff paste. A mortar that does not flow around the bar can leave voids at the interface, and the cement mortar, unlike the grout, was not designed to flow. Void formation was not examined, so this too is a hypothesis; it would be consistent with the poor showing of mortar (mean 0.021 MPa). Studies of grouted bars have concentrated on confinement by ducts and sleeves [19, 20], whereas the present cubes offered a cover of only about 69–72 mm, and the grout results should not be carried over to confined connections.

## 4.2 Nominal strengths, curing, and the strength trend

Epoxy bond stress increased with nominal strength, in line with the square-root dependence of bond on concrete strength that Ahmed et al. reported for post-installed ribbed bars in epoxy [13]. Their bars were ribbed and their concretes considerably stronger than ours, so we do not compare absolute values. Grout showed no strength trend, which would fit a capacity set at the steel–grout interface (the same grout was used in every mixture) and not at the grout–concrete interface; we did not test this. Bond–slip models for concretes of different strengths exist [39], but applying them would need measured strengths and complete load–slip curves, neither of which we have.

The weak point is what “strength” means here. All three concretes came from one dry-mix product; the 14.7 and 23.5 MPa mixtures differ in curing period only (Table 2), and the 4.9 MPa mixture is a sand-diluted version of the same product. Their true strengths may be closer than the labels suggest, in which case the step from 14.7 to 23.5 MPa is a curing effect and not a strength effect. Longer curing does not necessarily raise bond either: Fu and Chung reported that the bond of steel rebar decreased with increasing curing age [40]. The strength trends above are therefore trends across three batches and curing regimes, ordered as they are labelled.

## 4.3 Diameter, hole clearance, and the limit set by the bar

Epoxy bond stress rose with diameter (Section 3.3), and peak load scaled with an exponent of 2.1 ± 0.9, well above the value of 1 that a uniform interface stress implies. Three explanations are possible and the data cannot separate them. First, the clearance between the bar and the hole wall was not recorded, and if it changed with bar size the epoxy layer would have differed in thickness from one diameter to the next. Second, the ratio le/db falls from 23.3 to 11.7 between RB6 and RB12, and average bond stress over a long embedment is expected to be lower than over a short one if bond stress is not uniform along the bar. Third, bar capacity may have set the limit for part of the series: several RB6 specimens and the RB12 bars at 23.5 MPa reached bar stresses above the catalogue yield level (Section 3.4), which would flatten the gain with strength and distort the diameter trend.

Two points follow for the interpretation of τ. The RB12 epoxy result at 23.5 MPa (mean bar stress 244 MPa) sits at the catalogue yield level, so the bar and not the interface may have limited the load, and the reported 5.23 MPa is a lower bound on interface strength. One recorded failure also needs checking: the RB12 epoxy group at 4.9 MPa was logged as pull-out with bar yielding at a bar stress of 146 MPa (specimen RB12-5; group mean 122 MPa), which is well below the catalogue yield of 235 MPa, so either the recorded mode or the peak load is in error, or the bar was weaker than specified. [TO CONFIRM against the test notebook or the load record.]

## 4.4 What limits the capacity of GFRP bars in weak concrete

The GFRP results raise a more specific problem. Peak load did not grow from 14.7 to 23.5 MPa and, at 14.7 MPa, did not depend on diameter (Section 3.6). If bond were a uniform interface stress, P would be proportional to db (b = 1) and would increase with concrete strength. Instead, the exponent was 0.47, 0.01, and 0.41 at the three strengths (pooled 0.30, 95% half-width 0.12). Table 10 sets out six explanations and what the data can say about each; the first three concern the concrete and cannot be told apart without measured strengths and batch records.

Table 10. Possible reasons for the load plateau of GFRP bars at 14.7 and 23.5 MPa.

| Explanation | What the data show | Status |
| --- | --- | --- |
| 1. Nominal strengths differ from actual strengths | The 14.7 and 23.5 MPa mixtures differ in curing period only, and no cubes were crushed. | Plausible; cannot be tested without cube results |
| 2. A cube or splitting ceiling | Splitting occurred in 9 of 15 specimens at both 14.7 and 23.5 MPa, but peak load did not depend on failure mode (p = 0.72). | Not excluded; a ceiling set by concrete tensile strength would fall under explanation 1 |
| 3. Batch, age, or curing effects | Cubes came from separate batches; dates, ages, and immersion periods are not documented. | Cannot be tested from the records |
| 4. Random scatter alone | The change from 14.7 to 23.5 MPa was −1.05 kN (Welch p = 0.30, g = −0.38), so the plateau is an absence of a detectable rise. | Compatible with the data |
| 5. A limit at the grip | Individual peaks reached 25.8 kN (12 mm, 23.5 MPa), so one fixed grip ceiling near 21 kN is unlikely; a diameter-specific limit cannot be excluded. | Unlikely as a single ceiling; grip details needed |
| 6. Bar tensile capacity | Nominal stress at the maximum load was 786, 380, and 228 MPa for the 6, 9, and 12 mm bars; tensile properties were not measured. | Cannot be judged for the 6 mm bar; less likely for 9 and 12 mm |

What the data do establish is that the apparent stress τ = P/(πdble) is not a size-independent property in this test. At 14.7 MPa a 6 mm bar showed an apparent stress of 8.1 MPa and a 12 mm bar 4.1 MPa. A bond stress measured on one diameter should therefore not be applied to another, and a √f′c scaling should not be assumed in concrete this weak.

## 4.5 GFRP bars against the design expression

The ACI 440.1R-06 expression predicts an N that is independent of strength and rises slightly with diameter (0.99 to 1.19), whereas measured N fell with both (Table 9). The measured-to-predicted ratio decreased with diameter at every strength, from 1.42–2.15 for the 6 mm bars to 0.79–1.10 for the 12 mm bars, so the expression does not capture the size dependence seen here. Agreement should not be expected in any case, because the specimens have a bonded length of 12 to 23 bar diameters and concrete weaker than any GFRP test we found (the lowest was 20.4 MPa [34]), and the comparison is descriptive.

## 4.6 Test method and bonded length

The specimen follows a withdrawn standard [37] and departs from the pull-out specimen of ACI 440.3R-04, Annex B.3, which specifies a 200 mm cube and a bonded length of five diameters [38]. With le/db between 11.7 and 23.3, bond stress along the bar is unlikely to be uniform, and the reported τ is a long-length average that will sit below local peak values. Pull-out and beam tests also differ: in a recent comparison on ribbed GFRP bars, beam tests gave bond strengths roughly a quarter higher than pull-out tests [41], and RILEM beam tests are now used for steel and FRP bars in the same programme [42]. The two nearest active standards do not match our geometry, since ASTM A944 covers beam-end specimens of deformed bars [43] and ACI 355.4-19 covers the qualification of adhesive anchors [44]. The values reported here are comparable across our own groups, but they are not transferable to code checks.

[REVISION – reviewer comment 4] After the short-embedment series (Table S4) is tested, add here a comparison of the long-length average τ with the 5 db values, and reword the last sentence of this paragraph accordingly.

## 4.7 Implications for practice

The following points are our recommendations, drawn from the data but not themselves tested. Cement mortar should not be used to anchor plain bars in weak concrete: no mortar specimen exceeded 0.27 MPa, and 36 of 45 recorded zero load. Non-shrink grout reached a mean of only 0.43 MPa, and the within-group coefficient of variation had a median of 85% across the 7 groups with a non-zero mean, so a design value would have to be a lower characteristic value and not the mean. Even epoxy is a poor anchor for plain bars in the weakest concrete: it gave a mean of 1.0 MPa at 4.9 MPa and left 5 of 15 specimens without measurable resistance, so mechanical anchorage would be needed there. Epoxy is the only agent that gave a sizeable and strength-dependent bond at 14.7 MPa and above, and at RB12 and 23.5 MPa it loaded the bar to about its catalogue yield. For GFRP bars cast into weak concrete, capacity in this set-up was about 21 kN whatever the diameter, so neither a bond stress from one diameter nor a strength-proportional scaling should be assumed without a test on the actual bar.

## 4.8 Limitations

Concrete strength. Strengths are nominal grades, and two of the three mixtures differ only in curing period (Section 4.2). Sample size and records. Groups contain five specimens; failure mode was recorded for one specimen per plain-bar group; and the origin of the fifth plain-bar specimen and of the repeated GFRP tests is to be confirmed (Section 2.1). The very small coefficients of variation of some GFRP groups at 4.9 and 14.7 MPa should be checked against the raw load records. Installation. Hole diameter and clearance, cleaning, filling, water–powder ratios, loading rate, and test age are not documented, and the clearance may covary with bar diameter (Section 4.3). Bar properties. The yield strength of the steel bars was not measured, so the bar-stress screening in Section 3.4 rests on a catalogue value, and the tensile properties and surface type of the GFRP bars are undocumented. Series differences. The GFRP bars were cast in and the plain bars post-installed, so the two series are compared descriptively only. Test geometry. Section 4.6 describes the departure from current pull-out specimens. Analysis. The analysis plan was formed after the data were seen, and no multiplicity correction was applied. Literature. Our statements about the absence of comparable studies rest on a targeted, non-systematic search. [REVISE this limitation if the companion-cube results (Table S1) are adopted.]

# 5. Conclusions

Pull-out tests on 180 specimens in concrete of nominal strength 4.9–23.5 MPa support the following conclusions, each subject to the limitations in Section 4.8.

(1) For post-installed plain steel bars, the bonding agent explained most of the variation in bond stress (ηp2 = 0.73). Epoxy averaged 1.88 MPa, non-shrink grout 0.43 MPa, and cement mortar 0.021 MPa. The ranking depended on strength (agent × strength F(4, 108) = 23.2, p < 0.001, unchanged under permutation, HC3 inference, transformations, and data subsets): epoxy exceeded grout by 1.13 and 2.76 MPa at 14.7 and 23.5 MPa, but could not be separated from it at 4.9 MPa.

(2) Cement mortar was ineffective: no specimen exceeded 0.27 MPa, and 36 of 45 recorded zero load. Zero load was also recorded for 16 of 45 grout specimens and 6 of 45 epoxy specimens.

(3) Epoxy bond stress rose with nominal strength (1.00 to 3.13 MPa) and, less regularly, with diameter (1.17 to 3.06 MPa from RB6 to RB12), while grout showed neither trend. At RB12 and 23.5 MPa the mean bar stress (244 MPa) was at the catalogue yield level, so the bond stress there is a lower bound on the interface strength.

(4) Cast-in GFRP bars carried a mean peak load of about 21 kN at 14.7 MPa whatever the diameter (6–12 mm), and the load did not rise at 23.5 MPa (21.3 versus 20.3 kN, p = 0.30). Apparent bond stress and normalised bond therefore fell with diameter, and the measured-to-predicted ratio against ACI 440.1R-06 ranged from 0.79 to 2.15. The data cannot separate an interface limit from a limit in the concrete or the test arrangement.

(5) The values are indicative and not design-ready. The next tests should measure concrete strength on companion cubes, record load–slip curves, measure bar yield strength, record hole clearance and cross it with bar diameter, examine fracture surfaces, document the GFRP bar properties, and use the pull-out geometry of ACI 440.3R-04 alongside beam tests.

# Declarations

CRediT authorship contribution statement. Piyarat Paoleng: conceptualization, methodology, formal analysis, writing – original draft. Siriphat Maneekeaw: methodology, validation, writing – review and editing. Sirisak Kongsomsaksakul: investigation, data curation, writing – review and editing. Krairoj Mahannopkul: formal analysis, visualization, writing – review and editing. Ittipon Meepon: conceptualization, supervision, project administration, writing – review and editing. [TO CONFIRM by all authors.]

Funding. The authors received no external funding for this work. [TO CONFIRM.]

Declaration of competing interest. The authors declare no competing interests. [TO CONFIRM.]

Data availability. Specimen-level peak loads for all 180 specimens (bar type, diameter, agent, nominal strength) can be provided as supplementary material or on request to the corresponding author. [TO CONFIRM: repository or supplementary file, and availability of the raw load–slip records.] [ACTION – reviewer comment 2: obtain the raw UTM/LVDT files before submission. If raw records cannot be produced, remove the affected groups; do not state that the records are available.]

Use of AI-assisted tools. An AI assistant (Claude, Anthropic) was used to help with language editing, statistical scripts, and figure drafting. The authors checked all data, analyses, and interpretations and take full responsibility for the content. [TO CONFIRM against the policy of the chosen journal.]

Acknowledgements. The authors thank the students who prepared and tested the specimens [names to be added with their written consent] and the Department of Teacher Training in Civil Engineering at KMUTNB for laboratory space and equipment.

# Appendix S. Revision placeholders (replace or delete before submission)

WARNING. Every number in Tables S1–S4 is an ILLUSTRATIVE PLACEHOLDER written to show the expected layout and a plausible order of magnitude for this type of test. The values were not measured, are not in the v2 manuscript or its source projects, and must not be cited, used in any calculation, or submitted. Replace them with laboratory results or delete the tables. Table S5 is a blank checklist and contains no data.

Table S1. [PLACEHOLDER VALUES] Compressive strength of companion 150 mm cubes at the age of the pull-out test (reviewer comment 1).

| Nominal grade (MPa) | Mixture | Curing (d) | Age at test (d) | n | Measured f′c, mean (SD) (MPa) | CV (%) | Measured / nominal |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 4.9 (50 ksc) | Dry mix + equal mass of sand | 5 | 8 | 3 | 5.8 (0.6) | 10.3 | 1.18 |
| 14.7 (150 ksc) | Dry mix | 7 | 10 | 3 | 13.4 (1.0) | 7.5 | 0.91 |
| 23.5 (240 ksc) | Dry mix | 14 | 17 | 3 | 17.9 (1.3) | 7.3 | 0.76 |

Age at test is curing period plus the 2–3 d between installation and testing recorded in Section 2.3 [TO CONFIRM]. Cube standard and loading rate: [TO CONFIRM].

Table S2. [PLACEHOLDER VALUES] Tensile properties of the SR24 plain round bars from coupon tests (reviewer comment 7).

| Bar | db (mm) | Nominal area (mm²) | n | Yield strength fy, mean (SD) (MPa) | Tensile strength fu, mean (SD) (MPa) | fu / fy | Elongation (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| RB6 | 6 | 28.3 | 3 | 352 (8) | 448 (6) | 1.27 | 26 |
| RB9 | 9 | 63.6 | 3 | 326 (6) | 441 (5) | 1.35 | 28 |
| RB12 | 12 | 113.1 | 3 | 305 (7) | 436 (6) | 1.43 | 30 |

Catalogue minimum values used in v2: fy = 235 MPa, fu = 385 MPa. Yield point method and gauge length: [TO CONFIRM].

Table S3. [PLACEHOLDER VALUES] Tensile properties of the GFRP bars (reviewer comment 7). Maximum observed loads are taken from Section 3.6 of the manuscript.

| Bar | db (mm) | Area (mm²) | ffu, mean (SD) (MPa) | Ef (GPa) | εfu (%) | Ffu (kN) | Max observed P (kN) | Max P / Ffu |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| GF6 | 6 | 28.3 | 1040 (36) | 46.5 | 2.24 | 29.4 | 22.23 | 0.76 |
| GF9 | 9 | 63.6 | 905 (31) | 45.8 | 1.98 | 57.6 | 24.18 | 0.42 |
| GF12 | 12 | 113.1 | 812 (28) | 45.1 | 1.80 | 91.8 | 25.76 | 0.28 |

Manufacturer, surface treatment, fibre content and resin: [TO CONFIRM]. Ffu = ffu × area. Test method for ffu and Ef: [TO CONFIRM].

Table S4. [PLACEHOLDER VALUES] Supplementary pull-out series with bonded length le = 5 db (reviewer comment 4). Plain bars are epoxy-anchored; nominal strength is used until Table S1 is replaced by measured values.

| Specimen | db (mm) | le (mm) | Nominal f′c (MPa) | n | Peak load P (kN) | τ = P/(π db le) (MPa) | Slip at peak (mm) | Failure mode |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| GF6 | 6 | 30 | 14.7 | 3 | 6.2 | 10.9 | 0.85 | Pull-out |
| GF9 | 9 | 45 | 14.7 | 3 | 12.5 | 9.8 | 1.10 | Pull-out |
| GF12 | 12 | 60 | 14.7 | 3 | 20.6 | 9.1 | 1.32 | Pull-out (2), splitting (1) |
| GF6 | 6 | 30 | 23.5 | 3 | 7.1 | 12.6 | 0.92 | Pull-out |
| GF9 | 9 | 45 | 23.5 | 3 | 14.5 | 11.4 | 1.21 | Pull-out |
| GF12 | 12 | 60 | 23.5 | 3 | 24.0 | 10.6 | 1.48 | Splitting (2), pull-out (1) |
| RB6 epoxy | 6 | 30 | 23.5 | 3 | 3.3 | 5.9 | 0.64 | Pull-out |
| RB9 epoxy | 9 | 45 | 23.5 | 3 | 8.1 | 6.4 | 0.77 | Pull-out |
| RB12 epoxy | 12 | 60 | 23.5 | 3 | 15.4 | 6.8 | 0.86 | Pull-out |

Peak load and τ are group means; P was computed from the listed τ so that the columns are mutually consistent. Specimen geometry, block size and loading rate: [TO CONFIRM against ACI 440.3R Annex B.3].

Table S5. Data-provenance checklist (reviewer comment 2). Blank template – no data have been entered.

| Item | Evidence needed | Status |
| --- | --- | --- |
| Fifth specimen of every plain-bar group | Specimen ID, casting date, test date, record of who tested it | To be completed |
| Repeated GFRP tests (25 of 45 values differ from the project report) | Both sets of values, reason for repetition, raw load files of both | To be completed |
| Raw load–slip files (UTM and LVDT export) | One file per specimen, with machine, rate and date | To be completed |
| Photographs and notebook pages | Time-stamped images of each batch and test | To be completed |
| GFRP coefficients of variation of 2–7% (Section 3.6) | Comparison against raw peak loads; explanation of low scatter | To be completed |
| Consent and data-sharing permission | Written permission from the students for data and photographs | To be completed |

# References

[1]	Zheng, Y., Fan, C., Ma, J. et al. Review of research on bond–slip of reinforced concrete structures. Construction and Building Materials, 2023, 385, 131437. DOI: 10.1016/j.conbuildmat.2023.131437.

[2]	Vembu, P.R.S. and Ammasi, A.K. A comprehensive review on the factors affecting bond strength in concrete. Buildings, 2023, 13 (3), 577. DOI: 10.3390/buildings13030577.

[3]	Xing, G., Zhou, C., Wu, T. and Liu, B. Experimental study on bond behavior between plain reinforcing bars and concrete. Advances in Materials Science and Engineering, 2015, 2015, 604280. DOI: 10.1155/2015/604280.

[4]	Darwin, D., Zuo, J., Tholen, M.L. and Idun, E.K. Development length criteria for conventional and high relative rib area reinforcing bars. ACI Structural Journal, 1996, 93 (3), pp. 347–359. DOI: 10.14359/9694.

[5]	ACI Committee 318. ACI 318-08: Building code requirements for structural concrete and commentary. Farmington Hills, MI: American Concrete Institute, 2008.

[6]	Opabola, E.A. Bond strength and development length models for straight plain longitudinal reinforcement in tension. ACI Structural Journal, 2022, 119 (6), pp. 165–175. DOI: 10.14359/51736111.

[7]	Marshall, J.D., Lang, A.F., Baldridge, S.M. et al. Recipe for disaster: construction methods, materials, and building performance in the January 2010 Haiti earthquake. Earthquake Spectra, 2011, 27 (S1), pp. S323–S343. DOI: 10.1193/1.3637031.

[8]	Yepez, F. and Yepez, O. Role of construction materials in the collapse of R/C buildings after Mw 7.8 Pedernales – Ecuador earthquake, April 2016. Case Studies in Structural Engineering, 2017, 7, pp. 24–31. DOI: 10.1016/j.csse.2016.12.001.

[9]	Tutu, K.A., Odei, D.A., Baniba, P. et al. Concrete quality issues in multistory building construction in Ghana: cases from Kumasi metropolis. Case Studies in Construction Materials, 2022, 17, e01425. DOI: 10.1016/j.cscm.2022.e01425.

[10]	Yuva, Y. Low-strength concrete properties in existing structures using NDT and core test results. Journal of Building Engineering, 2023, 76, 107281. DOI: 10.1016/j.jobe.2023.107281.

[11]	Jafari, A., Shahmansouri, A.A., Abdulridha, H.A. et al. Effect of CFRP confinement on bond-slip behavior of steel rebar in low-strength concrete: experimentation, prediction and parametric study. Construction and Building Materials, 2025, 477, 141333. DOI: 10.1016/j.conbuildmat.2025.141333.

[12]	Tayeh, B.A., EL dada, Z.M., Shihada, S. et al. Pull-out behavior of post installed rebar connections using chemical adhesives and cement based binders. Journal of King Saud University – Engineering Sciences, 2019, 31 (4), pp. 332–339. DOI: 10.1016/j.jksues.2017.11.005.

[13]	Ahmed, K.S., Shahjalal, Md., Siddique, T.A. et al. Bond strength of post-installed high strength deformed rebar in concrete. Case Studies in Construction Materials, 2021, 15, e00581. DOI: 10.1016/j.cscm.2021.e00581.

[14]	Fayed, S., Alkharisi, M.K., Bayoumi, E.A. et al. Bond of ribbed and threaded steel reinforcement bars post-installed in concrete considering bonded length and adhesive type. Scientific Reports, 2026, 16, 10762. DOI: 10.1038/s41598-026-42964-4.

[15]	Multani, A.S. and Gupta, P.K. Bond strength analysis of post-installed rebar with chemical adhesive in concrete mixed with marble powder and glass fiber. Journal of Adhesion Science and Technology, 2024, 38 (7), pp. 1014–1042. DOI: 10.1080/01694243.2023.2245590.

[16]	Hussein, D.A. and Sarkawt, S.A. Experimental investigation of post-installed anchors' behavior under axial tensile force. Polytechnic Journal, 2024, 13 (1), 22. DOI: 10.59341/2707-7799.1835.

[17]	Rosca, B. and Corobceanu, V. Mix design approach of supplementary cementitious materials Portland cement-based mortars for anchoring post-installed reinforcement bars into hardened concrete. Procedia Manufacturing, 2020, 46, pp. 186–193. DOI: 10.1016/j.promfg.2020.03.028.

[18]	Darwin, D. and Zavaregh, S.S. Bond strength of grouted reinforcing bars. ACI Structural Journal, 1996, 93 (4), pp. 486–495. DOI: 10.14359/9707.

[19]	Raynor, D.J., Lehman, D.E. and Stanton, J.F. Bond-slip response of reinforcing bars grouted in ducts. ACI Structural Journal, 2002, 99 (5), pp. 568–576. DOI: 10.14359/12296.

[20]	Ahn, B.-I., Kim, H.-K. and Park, B.-M. Confining effect of mortar grouted splice sleeve on reinforcing bar. Journal of the Korea Concrete Institute, 2003, 15 (1), pp. 102–109. DOI: 10.4334/jkci.2003.15.1.102.

[21]	Jia, J., Zhao, N., Bai, Y. et al. Bond-slip model for rebar mounted to high-strength grouting material. Journal of Building Engineering, 2023, 74, 106794. DOI: 10.1016/j.jobe.2023.106794.

[22]	Zhang, W., Jia, Y., Cen, Q. et al. Bond–slip constitutive relationship at the interface between reinforcing steel and grout in fully grouted sleeve couplers. Buildings, 2026, 16 (11), 2098. DOI: 10.3390/buildings16112098.

[23]	Liu, D., Liu, C., Zhang, H. et al. Optimizing machine learning with SSA and PSO for anchor bolt–grout bond strength prediction. Materials, 2026, 19 (5), 906. DOI: 10.3390/ma19050906.

[24]	Itoh, T., Ueda, R., Son, B. et al. Anchorage and bond strength of SBPDN bar embedded in high-strength grout mortar. Materials, 2026, 19 (1), 2. DOI: 10.3390/ma19010002.

[25]	Jia, Q. and Zhang, T. Microbial cement grout anchoring steel reinforcement pull-out test. Scientific Reports, 2024, 14, 1559. DOI: 10.1038/s41598-024-52196-z.

[26]	Achillides, Z. and Pilakoutas, K. Bond behavior of fiber reinforced polymer bars under direct pullout conditions. Journal of Composites for Construction, 2004, 8 (2), pp. 173–181. DOI: 10.1061/(ASCE)1090-0268(2004)8:2(173).

[27]	Baena, M., Torres, L., Turon, A. and Barris, C. Experimental study of bond behaviour between concrete and FRP bars using a pull-out test. Composites Part B: Engineering, 2009, 40 (8), pp. 784–797. DOI: 10.1016/j.compositesb.2009.07.003.

[28]	Wambeke, B.W. and Shield, C.K. Development length of glass fiber-reinforced polymer bars in concrete. ACI Structural Journal, 2006, 103 (1), pp. 11–17. DOI: 10.14359/15081.

[29]	Sólyom, S. and Balázs, G.L. Bond of FRP bars with different surface characteristics. Construction and Building Materials, 2020, 264, 119839. DOI: 10.1016/j.conbuildmat.2020.119839.

[30]	Yan, F., Lin, Z. and Yang, M. Bond mechanism and bond strength of GFRP bars to concrete: a review. Composites Part B: Engineering, 2016, 98, pp. 56–69. DOI: 10.1016/j.compositesb.2016.04.068.

[31]	Ekrami Kakhki, S.A. and Kheyroddin, A. Bond behavior of fiber reinforced polymer bars in concrete: a review. International Journal of Concrete Structures and Materials, 2025, 19, 120. DOI: 10.1186/s40069-025-00859-0.

[32]	Okelo, R. and Yuan, R.L. Bond strength of fiber reinforced polymer rebars in normal strength concrete. Journal of Composites for Construction, 2005, 9 (3), pp. 203–213. DOI: 10.1061/(ASCE)1090-0268(2005)9:3(203).

[33]	Islam, S., Afefy, H.M., Sennah, K. et al. Bond characteristics of straight- and headed-end, ribbed-surface, GFRP bars embedded in high-strength concrete. Construction and Building Materials, 2015, 83, pp. 283–298. DOI: 10.1016/j.conbuildmat.2015.03.025.

[34]	Shakiba, M., Hosseini, S.M., Bazli, M. et al. Enhancement of the bond behaviour between sand coated GFRP bar and normal concrete using innovative composite anchor heads. Materials and Structures, 2022, 55 (9), 236. DOI: 10.1617/s11527-022-02074-9.

[35]	ACI Committee 440. ACI 440.1R-06: Guide for the design and construction of structural concrete reinforced with fiber-reinforced polymer (FRP) bars. Farmington Hills, MI: American Concrete Institute, 2006.

[36]	Shbeeb, N.I., Katash, A.A., Oguzmert, M. et al. Estimation of the bond strength of fiber-reinforced polymer bars in concrete using artificial intelligence systems. Buildings, 2024, 14 (2), 369. DOI: 10.3390/buildings14020369.

[37]	ASTM International. ASTM C234-91a: Standard test method for comparing concretes on the basis of the bond developed with reinforcing steel (withdrawn 2000). West Conshohocken, PA: ASTM International, 1991.

[38]	ACI Committee 440. ACI 440.3R-04: Guide test methods for fiber-reinforced polymers (FRPs) for reinforcing or strengthening concrete structures. Farmington Hills, MI: American Concrete Institute, 2004.

[39]	Tang, C.-W. Modeling uniaxial bond stress–slip behavior of reinforcing bars embedded in concrete with different strengths. Materials, 2021, 14 (4), 783. DOI: 10.3390/ma14040783.

[40]	Fu, X. and Chung, D.D.L. Decrease of the bond strength between steel rebar and concrete with increasing curing age. Cement and Concrete Research, 1998, 28 (2), pp. 167–169. DOI: 10.1016/S0008-8846(97)00216-0.

[41]	Rahimi, M., Davoodi, M.R., Nematzadeh, M. et al. A comparative study between beam and pull-out tests on bond behavior of ribbed GFRP bar in concrete conforming to RILEM standards. Archives of Civil and Mechanical Engineering, 2025, 25, 37. DOI: 10.1007/s43452-024-01095-1.

[42]	Ekrami Kakhki, S.A. and Kheyroddin, A. Experimental investigation of bond behavior of steel, GFRP, and CFRP reinforcement in self-compacting and fiber-reinforced concrete using RILEM beam tests. Scientific Reports, 2026, 16, 19085. DOI: 10.1038/s41598-026-49366-6.

[43]	ASTM International. ASTM A944-10 (Reapproved 2015): Standard test method for comparing bond strength of steel reinforcing bars to concrete using beam-end specimens. West Conshohocken, PA: ASTM International, 2015.

[44]	ACI Committee 355. ACI CODE-355.4-19 (Reapproved 2021): Qualification of post-installed adhesive anchors in concrete and commentary. Farmington Hills, MI: American Concrete Institute, 2021.

# Appendix A. Bond stress of the plain-bar series by group

Table A1. Mean bond stress τ (SD) in MPa for each plain-bar group (n = 5).

| Bar | Agent | τ at 4.9 MPa | τ at 14.7 MPa | τ at 23.5 MPa |
| --- | --- | --- | --- | --- |
| RB6 | Epoxy | 0.17 (0.24) [3] | 1.15 (0.99) | 2.19 (1.41) [1] |
| RB6 | Non-shrink grout | 0.00 (0.00) [5] | 0.61 (0.64) [2] | 0.32 (0.29) [1] |
| RB6 | Cement mortar | 0.00 (0.00) [5] | 0.00 (0.00) [5] | 0.00 (0.00) [5] |
| RB9 | Epoxy | 0.20 (0.21) [2] | 2.02 (0.69) | 1.98 (0.67) |
| RB9 | Non-shrink grout | 1.07 (0.36) | 0.00 (0.00) [5] | 0.50 (0.11) |
| RB9 | Cement mortar | 0.00 (0.00) [5] | 0.10 (0.13) [3] | 0.02 (0.03) [3] |
| RB12 | Epoxy | 2.61 (1.27) | 1.33 (0.77) | 5.23 (0.67) |
| RB12 | Non-shrink grout | 0.57 (0.41) [1] | 0.50 (0.45) [1] | 0.29 (0.24) [1] |
| RB12 | Cement mortar | 0.00 (0.00) [5] | 0.01 (0.02) [3] | 0.05 (0.05) [2] |

The number in square brackets is the count of zero-load specimens in the group (of 5), shown only when greater than zero.